N10 GENERAL FIXTURES VANITY UNITS

To be read with preliminaries and general conditions

Supplier: Toilet Cubicles Ireland, Unit 15 Donore Business pk, Donore rd, Drogheda, Co Louth. Ph /fax 041-9818148 Email: info@toiletcubiclesireland.ie Web: www.toiletcubiclesireland.ie

Product reference: V1 vanity unit

Vanity top: 20mm high pressure laminate post formed top balanced on the reverse

Up stand: 100mm cove profile finished square edge

Apron: 200mm post formed profile down stand finished square edge

Core material: 18mm Moisture resistant 650kg/m3 chipboard to V313

Finish: Subject to HPL manufacturer selected

Colour:  HPL selection card

Edge treatment: Square edged lipped in matching HPL/PVC

Panels: 20mm HPL faced made to measure panels

Core material: 18mm Moisture resistant 650kg/m3 chipboard to V313

Finish: Subject to HPL manufacturer selected

Colour: Subject to HPL manufacturer selected

Edge treatment: Square edged lipped in matching HPL/PVC or post formed vertical edges

Accessories: Concealed Keku ‘lift off’ brackets.

Support system: Treated softwood framework, notched and screwed made to measure and site assembled.

Dimensions: Unless stipulated dimensions as the technical data provided for V1 vanity units

Other requirements: Cut outs for basins marked on site by builder